BARACADE WB244

Water Based Silane/Siloxane Penetrating Water Repellent Sealer for Concrete and Masonry Surfaces

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 1, 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2.0	PRODUCT

2.__	PENETRATING WATER REPELLENT SEALER

A.	Penetrating Water Repellent: Water Based, ready to use, silane/siloxane blend, penetrating, clear water repellant sealer designed for use on concrete and masonry surfaces.

1.	Viscosity		50 cps

2.	Flash Point:		200 Deg F.

3.	NCHRP No. 244 Reduction in Chloride Content

| Average” | 82% |
| --- | --- |
| Min. Required | 75% |

4.	NCHRP No. 244 Reduction in Weight Gain

| 21 Days | 85% |
| --- | --- |

5. 	Reduction in Water Absorption SS-W-110C  88%

6.	VOC’s		50 g/l

7.	Depth of Penetration: 3/8”

8.	Product:

- Euclid Chemical Company (The): Baracade WB 244 www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification.

PART 3.0	EXECUTION

3.___	SURFACE PREPARATION

A.	New concrete surfaces must be a minimum 21 days old at time of application.

B.	Surface shall be structurally sound, clean, dry, free of dust, dirt, paint, efflorescence, laitance curing compounds and other contaminants that will prevent the proper penetration of penetrating water repellent. A dry substrate is required for proper penetration of the sealer. Prior to application, joints or cracks must be properly sealed. If acid is used for cleaning, neutralize completely before application of penetrating water repellent.

3.___	PENETRATING WATER REPELLENT APPLICATION:

A.	Apply per manufacturer’s recommendations utilizing low pressure airless spray equipment.

1.	Actual coverage and number of coats to be determined by field test sample application and water absorption testing. Final approval by architect/engineer is required.