TAMMSCRETE

Vertical Single component, polymer modified, cementitious skim coat for filling bugholes, honeycombs, and other surface imperfections on concrete and masonry surface.  Capable of being applied from feather edge to 1/8” thick (1/4” when extended with sand).

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

PART 2.0:	PRODUCT

2.__	BONDING AGENT/PRIMER

{REPAIR NOTE 1: Optional Bonding Agents}

{Note to Specifier: Certain bonding agents, adhesives and primers can be used to enhance the bond of this repair mortar. If desired choose a recommended bonding agent/primer from the data sheet and insert here. (Note: Latex additives will increase the volumetric resistivity of the mortar making it no longer compatible with Galvanic Anode Protection}

{PRODUCT}

2.__	CEMENTITIOUS REPAIR MORTAR

A.	Vertical Cementitious Skim Coat: Provide single component, polymer modified, portland cement based, repair mortar designed to be applied applied by trowel from featheredge to 1/8” thick on vertical surfaces to fill bugholes, honeycombs, and other surface imperfections and provide smooth surface.

1.	Compressive Strength minimum per ASTM C 109

7 days		3,000 psi

28 days		4,500 psi

2.	Flexural Strength minimum per ASTM C 78

7 days		500 psi

28 days		750 psi

3.	Bond Strength per ASTM C 1042

7 day		1,000 psi

28 day		1,400 psi

4.	Product:

a)	Euclid Chemical Company (The); Tammscrete; www.euclidchemical.com

B.	Manufacturer shall have ISO 9001 Quality Certification. To ensure compatibility all admixtures shall be from the same manufacturer.

C.	To ensure compatibility bonding agent and curing compound if used shall be from same manufacturer as repair mortar.

{REPAIR CURING NOTE 1}

2.___	CURING

{Note to Specifier: Euclid Chemical suggests curing this repair mortar with a high solids curing compound. If desired choose a recommended product from the data sheet and insert here. Guide spec language for these products can be found by accessing each product separately through this web site. Be advised that liquid curing compounds are typically not compatible with future penetrating sealer, adhesives or coatings. If such treatments are intended the specifier should insert language for a dissipating resin curing compound such as KUREZ DR VOX, a removable curing compound such as KUREZ RC, or insert language for proper moisture retaining curing methods meeting ACI 308. Duration of such cure should be minimum 3 days.}

PART 3.0:	EXECUTION

3.___	SURFACE PREPARATION

{CONCRETE PREP AND CLEANING NOTE}

A.     Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, debris, loosened concrete, paint, oil, efflorescence, laitance, and other contaminants, and shall have a minimum Concrete Surface Profile CSP equal to that recommended by the repair mortar manufacturer per ICRI Guideline 310.2.

3.___	REPAIR MORTAR APPLICATION:

{CEMENTITIOUS SKIM COAT APPLICATION NOTE}

A.	Cementitious Skim Coat Application: Mix and apply cementitious skim coat per manufacturer’s recommendations within the open time of the product scrub coat or any bonding agents.

3.___	CURING

{REPAIR MORTAR CURING EXECUTION}

{Note to Specifier: Euclid Chemical suggests curing this repair mortar with a high solids curing compound. If desired choose a recommended product from the data sheet and insert here. Guide spec language for these products can be found by accessing each product separately through this web site. Be advised that liquid curing compounds are typically not compatible with future penetrating sealer, adhesives or coatings. If such treatments are intended the specifier should insert language for a dissipating resin curing compound such as KUREZ DR VOX, a removable curing compound such as KUREZ RC, or insert language for proper moisture retaining curing methods meeting ACI 308. Duration of such cure should be minimum 3 days.}