TAMOSEAL

Cement based waterproofing and decorative finish for concrete and masonry surfaces

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 1, 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

A.	Cementitious Coating Mock-Up:

1.	Prior to commencing cementitious coating application, prepare a minimum <<insert size>> full scale, reference mock-up of each type, [and][color][and][ texture] of cementitious coating surface for approval by Owner. Said reference mock-up shall be constructed in location designated by owner/architect, using the same equipment, tools and methods for installing all materials as will be used for the remaining work to be performed.

PART 2.0:	PRODUCT

{PRODUCT}

2.__	CEMENT BASED WATERPROOF COATING

A.	Cement based, polymer modified, coating designed to waterproof and decorate concrete and masonry surfaces. Material shall provide the following characteristics:

1.	Compressive Strength minimum per ASTM C 109

7 days	C.	4,500 psi

28 days	E.	6,400 psi

2.	Flexural Strength minimum per ASTM C 348

7 days	G.	350 psi

28 days	I.	810 psi

3.	Tensile Strength per ASTM C 190

7 day	K.	330 psi

28 day	M.	390 psi

4.	Absorption ASTM C 67

24 Hour Soak	4.4%

5 Hour Boil	3.9%

5.	Freeze Thaw Resistance ASTM C 672

Loss at 50 cycles	1.2%

6.	Durability Factor per ASTM C666

After 300 cycles		101.0

7.	Water Permeance ASTM E 514 (after coating leaking wall)

Extent of damp area: 72 hours	0.0%

Maximum Leakage: 1 hour	None

Leakage Rate: ml/hr		None

Permeance Rating		Excellent

8.	Fungus Growth: Fed Test 141 Method 6272….Resistant

9.	Weatherometer ASTM G96

6,000 Hours	No crazing, cracking, chipping or flaking. Light chalking and color change. No other deterioration.

10.	Product:

a)	Euclid Chemical Company Tamoseal modified with Akro 7T  www.euclidchemical.com

b)	Color: [White] [Oyster] [Grey] [To be chosen by architect from manufacturer’s list of special colors.]

B.	Manufacturer shall have ISO 9001 Quality Certification.

PART 3.0:	EXECUTION

3.___	SURFACE PREPARATION

{CONCRETE PREP AND CLEANING NOTE}

A.     Concrete Preparation and Cleaning: Areas to receive concrete repair shall be structurally sound and free from deteriorated concrete, dust, dirt, debris, loosened concrete, paint, oil, efflorescence, laitance, and other contaminants. New concrete and masonry must be cured 7 days before application of coating. Abrade the surface to provide an absorptive surface. Repair all surface defects including cracks and voids. Allow patches and other surface preparations to cure for 24 hours. Saturate surface dry (SSD) the substrate with potable water prior to coating application.

3.___	CEMENTITIOUS COATING APPLICATION:

{CEMENTITIOUS COATING APPLICATION}

A.	Cementitious Coating Application: Mix and apply 2 coats of cementitious coating per manufacturers recommendations.